| SPECIFICATION TEXT |  |  |  |
| --- | --- | --- | --- |
| PRODUCT | Clicwall | DATE | 7 October 2020 |

DESCRIPTION

Wall covering system composed of 10 mm (12 mm on request) PEFC-labelled MDF core, finished with a resistant melamine top layer and a resistant melamine counter layer.

This melamine faced panel is produced from 100% circular wood supplied from residual streams from the wood industry or timber offcuts from sustainable forest management and verge maintenance.

Each panel has a tongue on one long side and a groove on the other long side, enabling them to click into one another. This creates a virtually seamless joint on the basis of the UNILIN patented Uniclic system. The top and bottom are finished flat.

Clicwall is available in a wide range of designs:

- A choice of 137 UNILIN Evola decors, 12 of which are supplied from stock.

- 3 decors are available from stock for Clicwall FR

  - Clicwall FR satisfies Euro Class B-s2,d0. Euro Class B-s1,d0 on request.

- Other decors on request.

Clicwall Paint are panels finished with a paintable foil that can be painted, covered in wallpaper or printed.

Two certified non-bearing dividing walls result in European standard EI60 and EI30 respectively. The EI60 system configuration is also certified for an acoustic value of 48 dB (Rw (C-4; Ctr-11) = 52 dB).

Clicwall walls can be finished according to the user’s preferences with a range of flexible profiles, skirting boards or bespoke aluminium profiles.

DIMENSIONS

Standard gross dimension: 2,785 x 618 x 10 mm (H x W x D)

Standard net dimension: 2,785 x 600 x 10 mm (H x W x D)

High panel gross dimension: 3,500 x 618 x 10 mm (H x W x D)

High panel net dimension: 3,500 x 600 x 10 mm (H x W x D)

Other dimensions are available on request.

TECHNICAL SPECIFICATIONS

| Panels |  | EN13986 |  |  |
| --- | --- | --- | --- | --- |
| Bending strength (N/mm²) |  | EN310 |  | 22 |
| Modulus of elasticity (N/mm²) |  | EN310 |  | 2,500 |
| Tensile strength (N/mm²) |  | EN319 |  | 0.6 |
| Swelling after 24 hours (%) |  | EN317 |  | 17 |
| Formaldehyde content (mg/100 g dry) |  | EN120 |  | (E1) ≤8 |
| Clicwall and Clicwall Paint fire reaction (rating) |  | EN13986 (Table 8) |  | D-s2,d0 |
| Clicwall FR 10 mm fire reaction (rating) |  | EN13986 (Table 8) |  | B-s2,d0 |
| Clicwall FR 12 mm fire reaction (rating) |  | EN13986 (Table 8) |  | B-s1,d0 |
| Water permeability (µ) |  | EN13986 (Table 9) |  | 12 (wet)/20 (dry) |
| Sound insulation (dB) |  | EN13986 (Chp 5.10) |  | R= 13*lg(ma)+14 |
| Sound absorption (coefficient) |  | EN13986 (Table 10) |  | 0.10 (250 - 500 Hz)/0.20 (1,000 - 2,000 Hz) |
| Thermal conductivity (λ) |  | EN13986 (Table 11) |  | 0.1 |
| Biological sustainability (rating) |  | EN335-3 |  | Class 1 |
| Pentachlorophenol (PCP) content (ppm) |  | EN13986 (Chp 5.18) |  | <5 |
| MDF |  | EN622-2 |  |  |
| Tolerance at average density (%) |  | EN323 |  | ±7 |
| Density (kg/m³) |  | EN323 |  | 760 |
| Moisture content (%) |  | EN323 |  | 6 ± 2 |
| Melamined panels | EN14323 |  |  |  |
| Thickness tolerance with respect to normal value (mm) | EN14323 |  | ±0.2 |  |
| Thickness tolerance (mm) | EN14323 |  | tmax-tmin ≤0.6 |  |
| Length tolerance (mm) | EN14323 |  | ±1 |  |
| Width tolerance (mm) | EN14323 |  | ±0.5 |  |
| Evenness (mm/lm) | EN14323 |  | ≤2 |  |
| Damage: short sides (mm) | EN14323 |  | <3 |  |
| Damage: tongue & groove (mm) | EN14323 |  | 0 |  |
| Surface flaws (points) (mm) | EN14323 |  | ≤2 |  |
| Surface flaws (lines) (mm/m³) | EN14323 |  | ≤20 |  |
| Resistance to scratches (N) | EN14323 |  | ≥1.5 |  |
| Resistance to stains (rating) | EN14323 |  | ≥3 |  |
| Resistance to fissures (rating) | EN14323 |  | ≥3 |  |
| Clicwall supplier | UNILIN |  |  |  |
| Tolerance at seamlessness (decor side) (mm) | UNILIN |  | <0.1 |  |